The design originally cam from  Alan Straniforth’s book “Race and Rally Car Source Book” (ISBN 0 85429 317 5) Haynes Publisher.

I have extended the original housing by 16 mm and moved the side arms of the wishbone out to the new length. I left the inside of the wishbone housing undersized so that after TIG welding the wishbone, I reamed the inside diameter to the required size (the TIG welding can sometimes lead to a small amount of distortion).

The main housing is made from  31.75 mm (1 1/8 ins) solid rod and the adjustment nut from 31.75 mm (1 1/8 ins) solid hex rod (measured from flat to flat)

If you are using the Transit rod end, the tapping hole is 16.5 mm (80% thread engagement from “Drills, Taps and Dies” by Tubal Cain - Workshop Practice Series number 12)  and use a 18 x 1.5 HSS tap using a good quality tapping paste.

The usual disclaimer applies to this design, Every attempt has been made to present a safe design but the author of the design cannot be held liable for any damage, injury or loss resulting from this design. If you have any doubts about making the component then it is recommended that you seek advice from a professional engineer.